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Sodium Metasilicate Cleaner CAS 10213-79-3


1. Sodium Metasilicate (Na2SiO3.nH2O) Basic Information:
	Item
	Sodium Metasilicate Anhydrous
	Sodium Metasilicate Pentahydrate
	Sodium Metasilicate Nonahydrate

	MF
	Na2SiO3
	Na2SiO3.5H2O
	Na2SiO3.9H2O

	MW
	123.07
	212.14
	284.2

	Melting Point
	1088°C
	72°C
	41.6°C

	CAS No.
	6834-92-0
	10213-79-3
	13517-24-3

	Density
	2.4g/cm3
	1.75g/cm3
	1.65g/cm3


 
2. Sodium Metasilicate (Na2SiO3.nH2O) Specification:
 
Sodium metasilicate anhydrous (Na2SiO3)
 
	Checking Item
	Test Standard (HG/T2568-94)

	Na 2 O%
	50.00-52.00

	SiO 2 %
	 
45.00-47.00

	Fe(ppm)
	≤200ppm

	Bulk density(g/cm3)
	1.05-1.35

	Particle Size%(18-60mesh)
	≥93.0

	Whiteness%
	≥85

	PH of 1.0% Solution
	12-13


 
 

Sodium metasilicate pentahydrate (Na2SiO3.5H2O)
	Checking Item
	Test Standard (HG/T2568-94)

	Na 2 O%
	28.00-30.00

	SiO 2 %
	27.00-29.00

	Fe(ppm)
	≤200ppm

	Bulk density(g/cm3)
	0.80-0.97

	Particle Size%(16-30mesh)
	≥90

	Whiteness%
	≥80

	PH of 1.0% Solution
	12-13


 
Sodium metasilicate nonahydrate (Na2SiO3.9H2O)
	Checking Item
	Test Standard (HG/T2568-94)

	Na 2 O%
	20.00-22.00

	SiO 2 %
	19.00-22.00

	Fe(ppm)
	≤200ppm

	Whiteness%
	≥70

	PH of 1.0% Solution
	12-13


 
Sodium Metasilicate Pentahydrate White Powder with CAS No 10213-79-3 
Packing
The inner bag is sealed PE plastic bag while the outer bag is tidely sutured plastic woven or kraft bag
Net weight: 25kg
Packed in accordance with the requirements.
 
Delivery 
Conveyance must be dry and clean. Handle with care and avoid breaking the bags by edged tools. Protect from rain-drenched and moisture.
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