厦门迪太进出口有限公司

XIAMEN DITAI IMP.& EXP. CO.,LTD

地址：中国厦门禾祥西路鸿升大厦8A

8FL, Hongsheng Building, West Hexiang Road, Xiamen, Fujian, China

TEL:0592-26808108 FAX:0592-2680880 E-mail: irene.zhang@xmditai.com

Sodium Metasilicate Cleaner CAS 10213-79-3

1. Sodium Metasilicate (Na2SiO3.nH2O) Basic Information:

| Item | Sodium Metasilicate Anhydrous | Sodium Metasilicate Pentahydrate | Sodium Metasilicate Nonahydrate |
| --- | --- | --- | --- |
| MF | Na2SiO3 | Na2SiO3.5H2O | Na2SiO3.9H2O |
| MW | 123.07 | 212.14 | 284.2 |
| Melting Point | 1088°C | 72°C | 41.6°C |
| CAS No. | 6834-92-0 | 10213-79-3 | 13517-24-3 |
| Density | 2.4g/cm3 | 1.75g/cm3 | 1.65g/cm3 |

2. Sodium Metasilicate (Na2SiO3.nH2O) Specification:

Sodium metasilicate anhydrous (Na2SiO3)

| Checking Item | Test Standard (HG/T2568-94) |
| --- | --- |
| Na 2 O% | 50.00-52.00 |
| SiO 2 % | 45.00-47.00 |
| Fe(ppm) | ≤200ppm |
| Bulk density(g/cm3) | 1.05-1.35 |
| Particle Size%(18-60mesh) | ≥93.0 |
| Whiteness% | ≥85 |
| PH of 1.0% Solution | 12-13 |

Sodium metasilicate pentahydrate (Na2SiO3.5H2O)

| Checking Item | Test Standard (HG/T2568-94) |
| --- | --- |
| Na 2 O% | 28.00-30.00 |
| SiO 2 % | 27.00-29.00 |
| Fe(ppm) | ≤200ppm |
| Bulk density(g/cm3) | 0.80-0.97 |
| Particle Size%(16-30mesh) | ≥90 |
| Whiteness% | ≥80 |
| PH of 1.0% Solution | 12-13 |

Sodium metasilicate nonahydrate (Na2SiO3.9H2O)

| Checking Item | Test Standard (HG/T2568-94) |
| --- | --- |
| Na 2 O% | 20.00-22.00 |
| SiO 2 % | 19.00-22.00 |
| Fe(ppm) | ≤200ppm |
| Whiteness% | ≥70 |
| PH of 1.0% Solution | 12-13 |

Sodium Metasilicate Pentahydrate White Powder with CAS No 10213-79-3

Packing
The inner bag is sealed PE plastic bag while the outer bag is tidely sutured plastic woven or kraft bag

Net weight: 25kg
Packed in accordance with the requirements.

Delivery 
Conveyance must be dry and clean. Handle with care and avoid breaking the bags by edged tools. Protect from rain-drenched and moisture.

​